## Slide 1
22.04.01 Materials Science and Engineering
DFT study of hydroxyl defects
in LiFePO4 and LiMnPO4 cathode materials
Student: Irina Varlamova
Research Advisor: Andriy Zhugayevych
Co-Advisor: Dmitry Aksenov
10 June, 2020

## Slide 2
Motivation
Positive electrode (cathode) in Li-ion batteries - Li(Fe, Mn)PO4
What is the structure of
hydroxyl point defects
?
MSU and Skoltech experimentalists [1]:
Obtained with hydrothermal synthesis from water solution
PXRD and Neutron Diffraction analysis - Li0.93Fe1.07P0.84O4
Infrared spectrum investigation showed OH peak
But the structure of OH defects remains unknown
IR
2
[1] Sumanov, V. D., Aksyonov, D. A., Drozhzhin, O. A., et.al. Chem.Mat., no.14(2019) 5035-5046.
Notes: Lithium iron phosphate is a widely used cathode material for the modern batteries, while lithium manganese phosphate is a prospective cathode material due to its high voltage. However it has low cycle stability. Recently the experiment with hydrothermal synthesis in water environment and investigation of properties were held. The electron diffraction analysis shows the deficiency of phosphorus. Infrared spectroscopy shows the weak peak of OH-bond within structure for non-concentrated solutions of samples (fig). But hydrogen bond presence in LiFePO4 is unknown and the structure of such defect has not been investigated yet. So, the main question of work is “What is the structure of hydroxyl point defects?”

## Slide 3
3
Structure under study
Tryphylite type structure with Pmna space group, similar to olivine (Mg2+, Fe2+)2SiO4
Notes: On this slide the schematic view of the structure under study is presented. The iron (or manganese) atom is located in octahedral environment of oxygen and has a brown color, phosphorus atom is located in tetrahedral environment of oxygen with purple color. The migration path of lithium during charge/discharge process is through b-axes, green color. Additionally, there are void polyhedral sites, which will be shown later.

## Slide 4
Aim and objectives
Aim
To determine the structure and formation energy of OH defects in Li(Fe,Mn)PO4 using density functional theory (DFT)
Objectives:
To study:
the energy and structure of OH defect in the tetrahedral and octahedral voids;
the energy and structure of Li/H and Fe/2H substitution defects;
the energy and structure of PO4/(OH)4 substitution defects;
the dynamics of OH defects in LiFePO4 at elevated temperatures
4
Notes: So, the main goal of current work is to determine the hydrogen defects structure in Li(Fe,Mn)PO4 using DFT approach. The main task is to study the energy and structure of OH defect in the void tetrahedral and octahedral sites and of Li/H and Fe/2H and PO4/(OH)4 substitution defects. Also the dynamics of OH defects at elevated temperatures was provided

## Slide 5
Methods
Aim | Calculation methods
Electronic structure | Density Functional Theory (DFT)
Atomic structure | PBE, 400 eV, k-spacing 0.3 A-1 in VASP package
 | Atomic and shape optimization at 7 fixed volumes [1]
Structure of OH defects | Potential energy scan (PES) on grid
Dynamics of OH defects | Ab-initio Molecular Dynamics in VASP up to 10ps
Deintercalation potential | Cluster expansion method (CLEASE software) [2] and enumerative scan of Li-vacancies
SIMAN
PYTHON BASED FRAMEWORK
[2] Chang, J. H., Kleiven, D., et.al. Journal of Physics: Condensed Matter, no.31(2019), 325901.
5
[1] https://github.com/dimonaks/siman/wiki.
Notes: The detection of hydrogen defects within lithium iron phosphate structure is difficult, the DFT method of study is used for this investigation. The python based framework of SIMAN was used to prepare calculations and provide their postprocessing. The calculations of DFT models are provided in the VASP code. Volume scan method was used to find the lattice constant. We used the method of potential energy surface scan based on SIMAN to identify hydrogen positions. Also the evolution of the system with high temperature was calculated using molecular dynamics method. At first, deintercalation process of lithium was investigated using CLEASE method of DTU energy developers. However, it was difficult for calculation due to the absence of convergence, and the study continued with SIMAN package, generating a set of structures with Li vacancies.

## Slide 6
Li(Fe,Mn)PO4: structure and electronic properties
LiFePO4 |  | 
 | Current | Ref.
a, Å | 10.33 | 10.32 [1]
b, Å | 6.01 | 6.01 [1]
c, Å | 4.73 | 4.69 [1]
Voltage, V |  | 3.4[2]
[1] Urusova V , Semkin MA, et al. Ferroelectrics, 509(2017):74–79
[2] Li, G., Azuma, H., et.al. Electrochem. and Solid State Lett.no.5 (2002) A135.
LiMnPO4 |  | 
 | Current | Ref.
a, Å | 10.56 | 10.45 [1]
b, Å | 6.15 | 6.10 [1]
c, Å | 4.79 | 4.74 [1]
Voltage, V |  | 4.1[2]
Tryphylite type structure with Pmna space group, similar to olivine (Mg2+, Fe2+)2SiO4
6
Notes: Both materials have a triphilite structure, which is quite similar to the olivine group. Minerals of this group are common materials of earth mantle. Forsterite is more investigated and is a widely studied material in terms of defects presence. The calculations of the current work with GGA-PBE potential and the reference values of lattice parameters are presented in the tables. According to this comparison, the structure characteristics can be successfully predicted in GGA approximation.

## Slide 7
7
Structure of LiFePO4 and P vacancy
Unit cell of LiFePO4 in polyhedral representation → different nonequivalent positions of interstitial or substitutional hydrogen defects
(hydrogen goes into tetrahedral voids)
Notes: The unit cell of lithium iron phosphate has the structure, which is presented on this slide. This structure in polyhedral representation has 8 octahedral sites of Li and Fe in oxygen environment and 4 tetrahedral sites of P positions. As it will be important for further narration, I will consider the environment of this P: it will be 5 iron octahedral and 4 lithium octahedral and several empty regions. Thus, using this structural information we can consider possible positions of H defect within structure.

## Slide 8
8
Types of OH defects in LiFePO4
More stable from:
Mössbauer analysis
Comparison with other defects
Comparison with PO4/OxH4 (x<4)
P vacancy site
Interstitial H in
tetrahedral void
Interstitial H in
octahedral void
Li(Fe,Mn)PO4 with 25% OH
Substitution of Li by H
Substitution of Fe by 2H
2.96 eV
2.76 eV
0.89 eV
0.88 eV
PO4/(OH) 4 0.53 eV
Notes: Many localization options of OH bond can be found within LFP structure. Interstitial H defect can be localized in the void octahedral or tetrahedral site. Additionally, the substitution of Li, Fe or P by hydrogen can be observed. All interstitial defects and substitution of Li or Fe by Hydrogen provided high formation energy and non-stable structure. In this work we will consider the substitution of P by four H defects.

## Slide 9
9
Structure of OH defects in Li(Fe,Mn)PO4
HIGH
Energy
(16.3 eV)
LOW
Energy
(-1.5 eV)
Notes: On this slide the representative of Potential Energy Surface scan method is shown. The central yellow area is a phosphorus vacancy tetrahedral site. The hydrogen positions relative to each of oxygen atoms were considered as a cloud in the general view. The color of each hydrogen position corresponds to its formation energy. The dark blue color is a more prospective position, which is chosen for the next step of PES. Choosing the low energetic position for each step, we found the most stable configuration and, as a result the stable defective structure.

## Slide 10: Structure of LiFePO4 with H defects
10
Unit cell of LiFePO4 with 25% OH with phosphorus vacancy on tetrahedral site LiFePO4 was created
There were four stages of the hydrogen distribution study: around each of oxygen in the phosphorus vacancy site (yellow triangle)
Initial structure
Final structure
Notes: After PES process, the equilibrium positions of hydrogen defects within phosphorus vacancy site was found. Structures with this localizations of hydrogen atoms have the smallest energy after relaxation and can be considered as an equilibrium. The next slide demonstrates three possible configurations.

## Slide 11
11
Structure of Li(Fe,Mn)PO4 with H defects
LiFePO4
LiMnPO4
PES method shown possible configurations of OH defects within Li(Fe,Mn)PO4
E, eV
0
0.1
1.22
0
0.02
0.08
0.99 Å
0.99 Å
1.00 Å
0.99 Å
1.77 Å
1.82 Å
0.98 Å
1.00 Å
0.98 Å
2.21 Å
1.85 Å
LiFePO4
LiMnPO4
Notes: The same PES study of hydrogen position within phosphorus defective tetrahedral site was provided also for LiMnPO4. The three possible low energetic structures of Li(Fe and Mn)Phosphate with substitution of phosphorus by four hydrogen are presented on this slide. The main result is that each hydrogen creates the covalent 1A bond with its neighboring oxygen. Three of hydrogen atoms are localized in the vacancy tetrahedron when fourth hydrogen atom is located outside of vacancy site.

## Slide 12
13
Dynamics of OH defects in LiFePO4, 600 °C, 2ps
Also Molecular dynamics investigation:
T = 100, 400, 600, 800 °C
Molecular Dynamics study is necessary for complete investigation of possible PO4/(OH)4 defects configuration
T = 600 °C – annealing
Each color is corresponded to each of the four OH groups in the tetrahedron.
Stable OH covalent bond and the absence of its breaking were observed.
The evolution of O-H distance over time
Notes: Molecular dynamics of evolution of hydrogen defects within LFP with 25% of defects structure was provided. Temperature of MD investigation was chosen according to the annealing process in the synthesis conditions. In this case it is approximately 600°C. For this temperature we observed the change of defective structure with time.

## Slide 13
Though this is temperature is too high compared to experiment, it allows to reduce the simulation time
Such result is relevant requires longer simulation and calculations of barriers
Formation of temporal H2O molecule
(50% times)
Dynamics of OH defects in LiFePO4, 1100 °C, 2ps
14

## Slide 14
15
Such result requires longer simulation and calculations of barriers
Formation of H2 molecule
H-H distance 0.7 Å
Evolution of OH defects in LiFePO4, 600 °C
Notes: Additionally, we provided the MD study with 6.25% of defect concentration, where the existing of H2 molecule was observed also after relaxation of structure with 0K. This is an interesting result, which will be taken into account in the further investigation of energy barriers of h defects.

## Slide 15
16
Evolution of OH defects in LiFePO4
Hydrogen atom always forms a covalent bond with oxygen with 1Å length
The hydrogen molecule H2 is observed with bond length corresponding to vacuum value (0.74Å)
H-H 0.85 Å
H-H 0.70 Å
O-H distances, Å
O1-H
O2-H
O3-H
Notes: The evolution of hydroxyl defect at the certain temperature shows the existence of hydrogen bond with the neighboring oxygen. In the first diagram the conclusion about the absence of free hydrogen atom in the structure can be made. Each hydrogen atom always constructs the bond either with neighboring oxygen. On the other hand, the hydrogen atom can create the bond with Fe or the second H. These bonds are confirmed by H-H distance diagram, where the distance between two hydrogen atoms is equal 0.7 A, which corresponds to H2 molecule, and 0.85A, which corresponds to the H-Fe bond.

## Slide 16
17
Conclusion
Main results:
The energy and structure of interstitial H as well as substitutional Li/H, Fe/2H, and PO4/(OH) 4 defects in Li(Fe,Mn)PO4 were determined with DFT calculations.
The PO4/(OH) 4 defect has the lowest formation energy per H atom among all considered defects.
In PO4/(OH) 4 defect four H atoms form covalent bonds (~1 Å) with O. Three OH bonds are directed inside the O4-tetrahedral void left after P removal, while the fourth OH is located in the neighborhood void tetrahedral site.
The stability of PO4/(OH) 4 defects was confirmed with ab initio molecular dynamics at temperatures up to 600 ℃.
At 600 ℃ temporal formation of H2 complexes inside PO4/(OH) 4 defects was observed.

## Slide 17
Acknowledgements
I express my gratitude to
Dmitry Aksenov
and
Andriy Zhugayevych
for their support and advice
19
18

## Slide 18
Thank you for your attention!

## Slide 19
Defects formation energy calculation (GGA+U)
A1
General formula:
U (Fe) = 4.0 eV
Defect type | Eform (GGA) | Eform (GGA+U)
Li/1H | 0.38 | 0.89
Fe/2H | 0.50 | 0.88
P/4H | 0.51 | 0.53
P/5H | 0.89 | 0.73

## Slide 20
A2
Different defect concentration values
Concentration of PO4/(OH)4 | Eform, eV
25% | 0.47
6.25% | 0.55

## Slide 21
The influence of substitution phosphorus by 1, 2, 3 or 4 hydrogen atom to electronic structure is presented in the following DOS diagrams. The absence of band-gap at the Fermi level can be observed, which shows the conductive features of defective material.
LiFePO4 with P vacancy
PO4/O4H1 defect
PO4/O4H2 defect
PO4/O4H3 defect
PO4/O4H4 defect
Electronic properties of LiFePO4 with PO4/O4Hx defects

## Slide 22
Electronic properties of LiFePO4 with PO4/O4Hx defects 6,25%
The influence of substitution phosphorus by 1, 2, 3 or 4 hydrogen atom to electronic structure is presented in the following DOS diagrams. The absence of band-gap at the Fermi level can be observed, which shows the conductive features of defective material.
LiFePO4 with P vacancy
PO4/O4H3 defect
PO4/O4H4 defect
PO4/O4H2 defect
PO4/O4H1 defect
A3
Notes: Influence of hydrogen defect to intercalation process of Li is important in case of electrochemical application. When deintercalation potential of Li atom from pure LFP material is approximately 4.07 eV the decrease of such potential can be observed with presence of hydrogen defects in distance between phosphorus vacancy and li vacancy approximately 5A. Thus, we can define the influence of hydrogen defects for intercalation process of lfp.

## Slide 23
E, eV
-201.4
-201.8
-202.3
Addition configurations of defect from MD
-202.50
-202.51
-201.28
PES results
MD study results
14
Notes: But now, using results after MD study, we found several type of stable positions of hydrogen within LFP and the conclusion about repeat of previous PES result can be clear seen, then new structures of defects are also observed.

## Slide 24
15
Discussion of results 1
PES method shown possible configurations of OH defects within Li(Fe,Mn)PO4
Structures of PO4/(OH)4 defects are similar with SiO4/(OH)4 Mg2SiO4 forsterite *
(Results of PES application are in good agreement with references [1])
Molecular Dynamics study is necessary for complete investigation of possible PO4/(OH)4 defects configuration
[1] Qin, Tian, et al. ”Ab initio study of water speciation in forsterite.” APS Meeting Abstracts. 2018.

## Slide 25
16
Comparison of results between PES and MD study provided following conclusions:
MD investigation showed the same structure with minimum of energy as PES
Additionally, MD study provided new configuration of PO4/(OH)4 defects with simple low-energy characteristic
High-temperature simulation showed configurations with water ??? molecule within structure
Discussion of OH dynamics

## Slide 26
The following parts should be accomplished
Thermodynamic analysis of all possible substitution and interstitial defects
the influence of PO4/(OH)4 defects on electronic structure;
Longer MD runs at 600 C
the influence of PO4/(OH)4 defects on hydrogen migration in LiFePO4;
18
the interaction between substitution of P by 4 H and electronic structure:
the absence of band-gap at the Fermi level

## Slide 27
12
Most stable PO4/(OH)4 defects obtained after adding 4th H
LiFePO4
LiMnPO4
E, eV
0
0.1
1.22
0
0.02
0.08
Structures of PO4/(OH) 4 defects are similar with SiO4/(OH) 4 Mg2SiO4 forsterite
Notes: This slide provides the information about localization of hydrogen substitution defects within phosphorus defective tetrahedral. After PES process the 3 structures of LFP and 3 structures of LMP were chosen. And, using this information, some intermediate conclusions can be made.